| Electrical characteristics |
| --- |
|  | Nominal voltage (V) 3.6 |
|  | Capacity at C/3 rate (Ah) 16 |
|  | Specific energy (Wh/kg) 85 |
|  | Energy density (Wh/dm3) 186 |
|  | Specific power (W/kg) 1350 |
|  | Power density (W/dm3) 2900 |

| Mechanical characteristics |
| --- |
|  | Diameter (mm) 47 |
|  | Height (mm) 178 |
|  | Weight (kg) 0.680 |
|  | Typical volume (dm3) 0.31 |

| Operating conditions |
| --- |
|  | Operating temperature range (°C) as given by the thermal management system - 20 /+ 55 |
|  | Transport or storage temperature range (°C) - 40 /+ 65 |
|  | Voltage limits : - In charge (V) - In discharge (V) 3.9 2.1 |